**SKY 24\*0,75mm**



Annealed electrolytic flexible copper conductor, class 5 according to Iec 228.

PVC insulations (PVC/D type). Conductors of this cable have been identified by numbers.

Numerical markings appears at least 25 times per meter.

PVC outer sheath (pvc/ST5) black color.Conductors are white color.

Nylon rope for easy pulling of the outer sheath of this cable is optional.Nylon rope doesnot effect the price.

|  |  |  |  |
| --- | --- | --- | --- |
| **DIMENSIONS** | | | |
| **Nominal Cross-Section** | **Width (mm)** | **Height (mm)** | **Weight (gr/m)** |
| 6x0.75 | 19 | 4.2 | 142 |
| 12x0.75 | 33.8 | 4.2 | 284 |
| 16x0.75 | 44.4 | 4.2 | 366 |
| 18x0.75 | 50.5 | 4.2 | 415 |
| 20x0.75 | 55 | 4.2 | 463 |
| 24x0.75 | 65.6 | 4.2 | 550 |
| 24x0.75 \* | 70.4 | 4.2 | 642 |
| 12x1 | 36.2 | 4.4 | 330 |
| 16x1 | 47.6 | 4.4 | 445 |
| 20x1 | 59 | 4.4 | 545 |
| 24x1 | 70.4 | 4.4 | 620 |
| 24x1 \* | 75.6 | 4.4 | 740 |